Text file for COILBLD2.GIF, graphical instructions for

construction of high performance 1/4 wave Tesla resonators.

4) Once the coil is wound, it is sealed to prevent corona leakage

and to help protect against electrical breakdown between turns.

Sealing also prevents the windings from loosening up on the coil

form. I use the same sealers mentioned earlier, those being

petroleum based polyurethane, or two-part clear epoxy paint.

Coats of sealer are applied with a brush or spray until there are

no ridges and valleys in the wire. In other words the coats must

build up until the wire is completely imbedded in sealer. A fan

and radiant heat source may be used as required to speed the cure

rate of the sealer. Rotating the coil on the winding spindle will

aid in obtaining a smooth coating that is free of runs and drips.

5) Two plastic disks are cut to match the ends of the coil form.

The plastic should be approximately the same thickness as the

coil form walls. Experience shows that plexiglas is both readily

available and works quite well in this application. Dry fit and

file the caps as necessary until a good match is made to the coil

form ends. I rough up, or score, the matching surface of the

plastic disks where they will be bonded to the ends of the coil

form. This provides a surface around the edges to give the epoxy

adhesive a bite.

6) Make sure all surfaces are dry, clean, and free of oil. Place

a bead of good quality clear two-part epoxy adhesive around the

top of the coil form, then cap the end of the coil with the

plastic disk. Weight the end cap down until the epoxy has cured,

then flip the coil over and repeat the procedure to cap the other

end. I will stop here to make an important note:

NO HOLES ARE EVER DRILLED INTO THE SIDEWALL OF THE COIL FORM!

WIRE IS NEVER ALLOWED TO ENTER INSIDE OF THE COIL!

Ideally the secondary coil should be hermetically sealed. This

prevents internal electrical breakdowns of the coil and prevents

the uptake of moisture into the coil form when PVC plastic pipe

is used. If holes are drilled into the coil sidewalls, and/or,

the wire is allowed to enter inside of the coil, then spark

lengths that exceed the length of the winding will almost surely

cause the coil to fail. Once a coil has failed in this manner it

is not repairable. One small hole may be drilled into the bottom

end plate to allow the air pressure to equalize, but under no

circumstances should any other holes be drilled.

COILBLD2.GIF      6/8/95           Graphics and text prepared by:

Richard T. Quick II

10028 Manchester Rd

Suite 253

Glendale  MO  63122  USA